## Slide 1
Graphene Failure
The predicted failure mode depends on the tensile state.
EV0002 · EV0045
Paper
Failure Mechanisms of
Graphene under Tension
Authors and journal
C. A. Marianetti & H. G.
Yevick · Physical Review
Letters 105 (2010)
Fig. 4(a). Maximum stable strain across tensile directions; regions differ in which
instability occurs first.
Notes: Paper: “Failure Mechanisms of Graphene under Tension,” C. A. Marianetti and H. G. Yevick, Physical Review Letters 105, 245502 (2010), DOI 10.1103/PhysRevLett.105.245502. The title is shortened for the cover; the full paper title and citation are shown below. Figure 4(a) is the paper’s loading-direction map.
Evidence: EV0002 · EV0045

## Slide 2
What limits near-ideal graphene?
The first failure mechanism under a generic tensile state was still an open question.
EV0057 · EV0033 · EV0004 · EV0002
The prior experiment and calculations probe different loading contexts.
Nanoindentation
Lee et al. strained graphene to failure under
conditions described as nearly ideal.
Uniaxial phonons
Earlier calculations found elastic instability
for armchair or zigzag loading.
Open question
Which instability occurs first for a generic
state of tension?
This study
Compare the elastic limit with a finite-wave-
vector K1 phonon instability.
Notes: The paper opens with two findings from different loading contexts: nearly ideal nanoindentation caused failure, while previous armchair/zigzag phonon calculations identified elastic instability. The authors ask which instability comes first for a generic tensile state. This comparison motivates the calculations; it does not claim that the experiment and calculations reproduce identical boundary conditions.
Evidence: EV0057 · EV0033 · EV0004 · EV0002

## Slide 3
How are both limits tested?
The workflow compares elastic instability with the K1-mode onset.
EV0004 · EV0009 · EV0017 · EV0025
1 · Strain states
Evaluate strain-dependent tensile response,
including equibiaxial loading.
2 · DFT forces
Generate strained-structure forces using the
local density approximation.
3 · Phonons
Calculate phonons with the displacement
method.
4 · Compare limits
Track the elastic instability against the K1-
mode onset.
Notes: DFT forces as a function of strain are used to assess elastic instability. Phonons are computed with the displacement method, with forces generated using DFT in the local density approximation. The calculation then compares the elastic and K1-mode limits across tensile states. See the cited evidence in the speaker-note footer for the source spans.
Evidence: EV0004 · EV0009 · EV0017 · EV0025

## Slide 4
When does the K1 mode soften?
Two calculations place K1 softening near ε_A ≈ 0.21.
EV0055 · EV0025
These are calculated thresholds for idealized equibiaxial loading, not measured breaking strains.
Phonon threshold
K1 softens at ε_A = 0.205–0.212 under
equibiaxial strain.
Independent check
Mode-energy analysis predicts ε_A = 0.213,
closely matching the phonon threshold.
Fig. 1. In-plane phonon branches under equibiaxial strain;
the K1 mode approaches instability at K.
Notes: Figure 1 shows significant softening of in-plane phonons under equibiaxial strain. The phonon calculation places the K1 soft mode at ε_A = 0.205–0.212. A separate mode-energy analysis predicts ε_A = 0.213. These are closely matching calculated thresholds, not a direct measurement of breaking strain.
Evidence: EV0055 · EV0025

## Slide 5
How can K1 softening reduce strength?
The authors link K1 softening to a structural transition and reduced strength in some tensile
states.
EV0031 · EV0034 · EV0032
Structural route
The authors infer that the deepening K1 double well
leads toward isolated hexagonal rings.
Strength implication
The K-cell stress drops near softening; the
proposed route can reduce strength.
Fig. 3. Nominal stress versus equibiaxial strain; the
K-cell response drops near K1 softening.
Notes: The paper reports that further strain deepens and widens the K1 double-well potential. It interprets the mode as a route toward isolated hexagonal rings and reduced strength. Figure 3 supplies the mechanical response: the K-cell stress curve drops near the K1 softening. Present the structural pathway as the authors’ interpretation, not as a directly imaged transition in this calculation.
Evidence: EV0031 · EV0034 · EV0032

## Slide 6
Tensile state selects the failure mode
Elastic instability governs regions I and III; the K1 mode occurs first in region II.
EV0029 · EV0045 · EV0002
Regions I and III
Elastic instability precedes the K1 mode.
Region II
The K1-mode instability arrives first; the
route changes with tensile direction.
Fig. 4(a). Maximum stable strain across tensile directions; regions I/
III are elastic-limited and region II is K1-limited.
Notes: The authors identify regions I and III as elastic-instability failure, where the elastic limit precedes the K1 mode. The complementary region is limited first by the K1 instability. They emphasize that equibiaxial loading follows a different route from the usual uniaxial armchair/zigzag case. Use the labels in Figure 4(a) when presenting the regions.
Evidence: EV0029 · EV0045 · EV0002

## Slide 7
Do orientation and shear matter?
Rotation and shear make only small changes to the predicted K1 onset, but the state map is
incomplete.
EV0049 · EV0024 · EV0046 · EV0005
Rotation and shear checks do not enumerate every possible tensile state.
Rotation
The 15° map stays within the original/rotated
envelope; orientations were sampled every 3°.
Shear and scope
Shear shifts K1 onset only slightly. Anisotropy
leaves some tensile states untested.
Fig. 4(c). At 15° rotation, the failure map remains
within the original/rotated envelope.
Notes: The coordinates were rotated in 3-degree increments; Figure 4(c) displays the 15-degree case. The rotated results remain within the envelope formed by the original and 15-degree curves. The authors report no qualitative shear-induced change and only small quantitative shifts to K1 onset. Because graphene is anisotropic, the paper notes that the orientation/shear enumeration is not exhaustive.
Evidence: EV0049 · EV0024 · EV0046 · EV0005

## Slide 8
Experiment vs prediction?
The measured nominal strain (0.225) is closer to the calculated elastic limit (0.216), but the
failure route remains unresolved.
EV0054 · EV0028 · EV0021 · EV0020 · EV0014
K1 stabilization is a proposed explanation, not a demonstrated mechanism.
Measured
Nanoindentation reports nominal
equibiaxial breaking strain 0.225.
Calculated elastic limit
The equibiaxial elastic-instability strain is 0.216.
Authors’ proposal
The K1 mode may be stabilized
during nanoindentation.
Possible differences
Indenter environment and strain construction may
affect the comparison.
Notes: Lee et al. report a nominal equibiaxial breaking strain of 0.225. The paper says this is in much better agreement with its calculated equibiaxial elastic-instability strain of 0.216. The authors suggest that K1 may be stabilized in nanoindentation, but they do not establish this. They identify possible differences involving the indenter environment and the experimental versus constructed equibiaxial strain state.
Evidence: EV0054 · EV0028 · EV0021 · EV0020 · EV0014

## Slide 9
Conclusions and limits
Tensile state selects whether elastic instability or a K1 soft mode limits strength.
EV0029 · EV0034 · EV0002 · EV0054 · EV0021 · EV0005
PaperWorkflow evidence coverage is under review; the paper also notes that rotation/shear sampling is not exhaustive.
Mode selection
Elastic failure in regions I/III; K1 soft-
mode failure in region II.
Open limits
Indentation leaves the route unresolved;
rotation/shear sampling is incomplete.
Fig. 4(a). The loading-direction map summarizes where elastic and
K1-mode instabilities occur first.
Notes: The paper’s central result is mode selection by tensile state: elastic instability in regions I/III and a K1 soft-mode route in region II. The authors connect K1 softening with a phase transition and reduced strength in some states. The nanoindentation comparison does not settle which route occurred. The paper says its orientation/shear treatment is incomplete. PaperWorkflow’s synthesis readiness also marks evidence coverage as review, so this deck should not be read as exhaustive coverage of all workflow facets.
Evidence: EV0029 · EV0034 · EV0002 · EV0054 · EV0021 · EV0005